RUGGED MULTI VEHICLE ATF

RUGGED MULTI VEHICLE ATF is a synthetic blend ATF that is designed for use in automatic transmissions in most domestic and import passenger cars and light trucks. RUGGED MULTI VEHICLE ATF provides superior thermal stability and anti-wear protection. Its frictional properties provide smooth shifting and excellent anti-shudder performance in a wide range of vehicles.

BENEFITS:

- Guarantees peak transmission performance during high temperature operation

- Excellent anti-wear protection; increases transmission life

- Outstanding oxidative stability, foam resistance and corrosion control

- Excellent shear stability to ensure a long service life

- Maximum protection for towing and severe service

- Improved shift quality

| TYPICAL PROPERTIES: |
| --- |
| Gravity, °API | ASTM D-287 | 31.5 |
| Flash, °C | ASTM D-97 | 250 min |
| Pour Point, °F | ASTM D-92 | -30 |
| Viscosity: |  |  |
| cSt @ 40 °C | ASTM D-445 | 51 |
| cSt @100 °C | ASTM D-445 | 7.3 |
| Viscosity Index | ASTM D-2270 | 150 |

A SUPERIOR PRODUCT BY COLORADO PETROLEUM 11-01-2015 TH

# Text boxes

*SFU at half of the recommended drain interval due to TES 295 being a PAO fluid

**Not SFU for V2 or Z3--no supporting data

***Not SFU for 236.6, 236.7, 236.8, 236.9, 236.12, 236.20 (CVT)

****Not SFU for M-1375.4

*****Not SFU for N402--insufficient extreme pressure agent

******Not SFU for 14C, 14E, 16N--no supporting data