### RUGGED ALL SEASON Synthetic Blend Motor Oils

RUGGED ALL SEASON Synthetic Blend motor oils provide excellent protection against engine wear, rust, corrosion, oxidation, and thermal breakdown.  It also includes a viscosity index improver and pour point depressant designed to provide maximum protection under extreme temperature and operating condition.  RUGGED ALL SEASON Synthetic Blend motor oils supply an extra margin of safety for passenger cars, light trucks, vans and SUV’s.

(Note: warranty protection requires following manufacturer’s recommended drain intervals and viscosity grade)

# Specifications:

- Surpasses API service classification SN.

- Meets or exceeds Energy Conserving, ILSAC GF-5

(SAE 5W-20, SAE 5W-30 & SAE 10W-30).

- Exceed car manufacturer requirements for maintaining warranty validity.

- Meets or exceeds the latest automobile manufacturer’s recommendations.

- Meets or exceeds Ford WSS-M2C945-A.

| TYPICAL PROPERTIES |
| --- |
| SAE grade |  | 5W-20 | 5W-30 | 10W-30 | 10W-40 | 20W-50 |
| Resource Conserving |  | YES | YES | YES | N/A | N/A |
| Gravity, ° API | ASTM D-287 | 33.4 | 30.2 | 29.8 | 29.2 | 28.5 |
| Flash, °F | ASTM D-92 | 403 | 410 | 410 | 410 | 410 |
| Pour Point, °F | ASTM D-97 | -33 | -32 | -29 | -30 | -20 |
| Viscosity: |  |  |  |  |  |  |
| cSt @ 40 °C | ASTM D-445 | 60 | 65.0 | 69.4 | 92.4 | 152 |
| cSt @ 100 °C | ASTM D-445 | 9 | 10.5 | 10.5 | 13.7 | 17.5 |
| Viscosity Index | ASTM D-2270 | 127 | 150 | 139 | 150 | 125 |
| CCS: |  |  |  |  |  |  |
| Cp @ -15 °C | ASTM D-5293 |  |  |  |  | 9500 max |
| Cp @ -25 °C | ASTM D-5293 |  |  | 7000 max | 7000 max |  |
| Cp @ -30 °C | ASTM D-5293 | 6600 max | 6600 max |  |  |  |

A SUPERIOR PRODUCT BY COLORADO PETROLEUM 03-23-2017 JDS