### Rugged HT Heat Transfer Oil

RUGGED HT Heat Transfer Oil is an extremely high viscosity index premium heat transfer oil with excellent stability. Rugged HT contains rust and oxidation inhibitors, a select anti-foamant and state-of-the-art, anti-wear chemistry. Rugged HT as meets or exceeds Denison HF-2 specifications.

Rugged HT was developed for extreme heat applications and climates. It offers an extra level of protection where heat transfer oils must provide for rapid water separation, extreme pressures and consistent viscosity control. Rugged HT contains anti-wear additives and is outstanding as a general purpose oil for machine tools, electric motors and other general lubrication points where oil is required.

Meets or exceeds:

Denison HF-O, HF-1, HF-2

Vickers Industrial & Mobile applications plus Sperry Vickers I-286-S

Cincinnati Milacron P-69

| TYPICAL PROPERTIES |
| --- |
| ISO grade |  | 46 |
| Gravity, °API | ASTM D-287 | 34.2 |
| Specific Gravity | ASTM D-4052 | 0.8540 |
| Flash Point °F | ASTM D-92 | 440 |
| Pour Point °F | ASTM D-97 | -23 |
| Viscosity, SUS |  |  |
| @ 100 °C | ASTM D-445 | 7.29 |
| @ 40 °C | ASTM D-445 | 45.8 |
| Viscosity Index | ASTM D-2270 | 121 |
| Rust Test | ASTM D-655 A&B | PASS |
| Demulsibility Test | ASTM D-1401 | PASS |

A SUPERIOR PRODUCT BY COLORADO PETROLEUM 08-09-2016JDS