# Rugged 400 Engine oil

## Rugged 400 Engine Oil meets all current emission standards.  Rugged 400 SAE 15W-40 meets the API classification CK-4/SN.  This oil is completely backwards compatible and allows fleets to use one product for newer engines as well as older units.  This high-grade oil is designed to meet the needs of engines using Selective Catalyst Reduction (SCR), Exhaust Gas Recirculation (EGR) systems, Diesel Particulate Filters (DPF’s), and Diesel Oxidation Catalyst (DOC’s). Rugged 400 Engine Oil is formulated to be used with Ultra Low Sulfur Diesel (ULSD) as well as normal / low sulfur diesel fuels.

RECOMMENDED:

- Supercharged or naturally aspirated diesel engines for which the manufacturer specifies series 3 (S-3) motor oil.

- Wherever a MIL-PRF-2104E, or a MIL 4652D motor oil is required.

- For API service SN/SM/SL/SJ/SH/CD-II/CD-4/CF/CF-II/CF-4/CG-4/CI-4/CI-4 Plus

CJ-4/CK-4(SAE 10W-30 & SAE15W-40).

- For API service CF, CF-2 (SAE10W & SAE 20)

- For API service CF, CF-2, SJ (SAE 30, SAE 40, SAE 50)

MEETS OR EXCEEDS REQUIREMENTS OF:

- MIL-PRF-2104E, MIL-L-2104F, MIL-L-4652D, HT/HS

- Cummins N.T.C. 400, Cummins bench test, CRC L-38, Cummins CES 20078, 20076, 20072 and 20071, 20081

- Caterpillar Superior Lubricants (Series 3), TO-2, Caterpillar ECF-1, Caterpillar 1-P, Caterpillar 1N @ 1M-PC, ECF-3

- Detroit Diesel 7Se-270, DDC 6V-92A, DDC Series 2000/4000 Category 1, DDC 93K218

- Ford WSS-M2C171-F1

- GM 6.2L

- MACK EO-O Premium Plus 07

- Allison C-4 (10 and 30),

- Mack T-8, Sequence IID, IIIE, & VE

- MTU 2.1

- Man 271, ACEA A3/B3/E2, 3275, E7

| TYPICAL PROPERTIES |
| --- |
| SAE Grade |  | 10W | 30 | 40 | 50 | 10W-30 | 15W-40 |
| Gravity, °API | ASTM D-287 | 30.0 | 29.0 | 28.0 | 28.0 | 29.8 | 28.5 |
| Flash, COC °F | ASTM D-92 | 406 | 450 | 493 | 514 | 410 | 439 |
| Pour Point, °F | ASTM D-97 | -25 | -05 | 0 | 8 | -29 | -25 |
| Viscosity |  |  |  |  |  |  |  |
| cSt @ 40 °C | ASTM D-445 | 41.7 | 102 | 156 | 245 | 69.5 | 101.5 |
| cSt @ 100 °C | ASTM D-445 | 6.61 | 12.0 | 15.0 | 20.0 | 10.5 | 14.6 |
| Viscosity Index | ASTM D-2270 | 110 | 107 | 96 | 94 | 140 | 144 |
| CCS, Cp @ -20 °C | ASTM D-5293 |  |  |  |  |  | 7000 MAX |
| Total Base Number | ASTM D-2896 |  |  |  |  |  | 10.0 MIN |
| Sulfated Ash, wt. % | ASTM D-874 |  |  |  |  |  | 1.0 MAX |

### A SUPERIOR PRODUCT BY COLORADO PETROLEUM 03 22 2017 JDS

# Text boxes

- Daimler-Chrysler 228.1 and 229.1, 228.31

- Volvo VDS-4

#### Global DHD-1

- EMA LRG-1,

- HTHS D4683 – 4.22 (SAE 15W-40)