# Rugged 400 SAE 5W-40 FULL SYNTHETIC

# Engine oil

Rugged 400 5W40 Full Synthetic Engine Oil Is fully formulated with synthetic base stocks, including PolyAlphaOlefin (PAO) synthetic base oil.  It provides improved fuel economy, compared to conventional SAE 15W-40 oils. API CK-4 represents the highest level of engine protection and performance ever built into a new lubricant specification. It was designed for all diesel engine applications, including today’s emission controlled engines with SCR, EGR and diesel particulate filters using Ultra-Low Sulfur Diesel fuel (<15 PPM Sulfur) (ULSD) and Low Sulfur Diesel (LSD). It is formulated to improve wear protection, deposit and oil consumption control, soot-related viscosity control, prevention of viscosity loss from shearing, used oil low- temperature pumpability and protection from thermal and oxidative breakdown. It is suitable for use in almost all foreign and domestic diesel engines for both the latest 2007 emission compliant and older engines.  Always consult your owner’s manual for proper application.

ATTRIBUTES:

- Excellent soot disbursement with viscosity control.

- Improved fuel economy, compared to conventional SAE 15W-40 motor oils.

- Exceptional wear protection for longer engine life.

- Superior low temperature properties improves cold starting.

- Year-round formula for extreme hot and cold temperatures.

MEETS OR EXCEEDS REQUIREMENTS OF:

- API CK-4, CJ-4, CI-4 PLUS, CH-4, CG-4, CF/SN, SM, SL

- Caterpillar ECF-1a, ECF-2, ECF-3

- Volvo VDS-4, VDS-3 X DDC Power Guard 93 K218

- DDC/MTU Series 2000/4000 1 and 2 engine performance

- Cummins CES 20081, 20077, 20076

- Mercedes Benz 228.31

- Mack EO-O Premium Plus, Mack EO-N Premium Plus 03, EO-N Premium Plus, EO-M Plus, EO-M

| TYPICAL PROPERTIES |
| --- |
| SAE Grade |  | 5W-40 |
| Gravity, °API | ASTM D-287 | 29.8 |
| Flash, COC °F | ASTM D-92 | 410 |
| Pour Point, °F | ASTM D-97 | -27 |
| Viscosity Cst @ 40 °C | ASTM D-445 | 88.8 |
| Viscosity Cst @ 100 °C | ASTM D-445 | 14.5 |
| Viscosity Index | ASTM D-2270 | 170 |
| CCS, cP @ -30 °C | ASTM D-5293 | (6600) MAX |
| Total Base Number | ASTM D-2896 | 11.0 MIN |
| Sulfated Ash | ASTM D-874 | 1.0 MAX |

### A SUPERIOR PRODUCT BY COLORADO PETROLEUM 12-18-2017 JDS

# Text boxes

- MAN 3275

- DHD-1, ACEA E7 and E5

- Allison C-4

- Global DHD-1

- JASO DH-2

- Renault RLD-3